## Slide 1: High-throughput evaluation of SOFC electrode material composition gradients
A case study with La0.6Sr0.4Co1-xFexO3-δ
Chris Kucharczyk Group Meeting Dec. 12 2016

## Slide 2: Administrative notes
Shared files (e.g. group presentations) are migrating to box.northwestern.edu
  Create an account ASAP so I can share group folders with you

## Slide 3: Motivation
Solid oxide fuel cells are good:
  efficient, fuel flexible, cheap material construction
Cathodes are bad:
  high polarization resistance
  low power density
  require high temperatures and expensive material construction
Research aims:
  Understand what makes a cathode material “good”
  Discover new, better cathode materials faster

## Slide 4: Approach: Northwestern/UMD Collaboration
H. Koinuma and I. Takeuchi, Nature Materials (2004)
electrolyte (YSZ, BZY…)
electrode film
Pulsed laser deposition (PLD) with motorized shutter | Photolithography + ion milling | Environmental scanning electrical impedance probe
Generate dense gradient oxide films | Pattern precise gradient geometries | Measure impedance spectra and extract meaningful material parameters
electrolyte (YSZ, BZY…)
porous, high-activity counterelectrode
Heated stage
Al2O3

## Slide 5: Microelectrode impedance spectroscopy
 Attribute large ressitance, low-frequency processes to microelectrode
Nyquist plot
  Resolve features with different time constants
electrolyte (YSZ)
porous, high-activity counterelectrode
10 kHz to 3 mHz
Pt-Ir probe tip
tip diameter
Extract information by fitting to a model circuit
Uniform gas environment
Decreasing ω
Electronically isolated electrodes

## Slide 6: Mixed-conducting microelectrode circuit model
Model processes as resistances and capacitances
Model mixed conduction as rails coupled by
Surface
Bulk
Interface
Electrolyte
Counterelectrode
Ions
Electrons
dCchem
After J. Jamnik & J. Maier. PCCP (2001),
W. Lai & S. M. Haile. PCCP (2005),
and W. Chueh, Caltech Thesis
dRion
dReon

## Slide 7: Simplifying properties
Surface
Bulk
Interface
If Cchem >> Cint, Csurf, C ~ Cchem
Scaling of these fitted parameters with geometry gives clues as to the dominant mechanisms at play

## Slide 8: Why this approach is useful
Multiple gradients (composition, diameter, thickness…) in multiple environments yields rich electrochemical information
  Diameter or thickness variation  electrochemical pathway
  Composition variation  optimization
  Oxygen atmosphere variation  nonstoichiometry
  Temperature variation  Arrhenius behavior
2PB pathway
3PB pathway
W. C. Chueh & S. M. Haile. Annual Review of Chemical and Biomolecular Engineering (2012)

## Slide 9: Case Study: La0.6Sr0.4Co1-xFexO3-δ
Microdot
diameters
500µm
300µm
200µm
150µm
125µm
100µm
100µm

## Slide 10: Nyquist and bode plots
LSC
LSF
750°C
1 atm O2
750°C
1 atm O2

## Slide 11: Resistance and capacitance
750°C
1 atm O2
100-500µm microdots
LSC
LSF
x 4 temperatures!
x 5 pO2 atmospheres!

## Slide 12: Geometric dependence
775°C
1 atm O2
775°C
0.2 atm O2
A slope of ~-2 suggests we are, indeed, 2PB limited
As expected, capacitance scales with dot area
LSC
LSF

## Slide 13: Atmosphere dependence
750°C
-0.5 < slope < -0.75  diatomic oxygen likely involved in rate-determining step (Chueh 2012)
Power law fitting can obtain absolute oxygen non-stoichiometry
LSC
LSF
750°C

## Slide 14: Arrhenius behavior
LSC
LSF

## Slide 15: Temperature dependence
Can see onset of oxygen vacancy creation!
LSC
LSF

## Slide 16: Mizusaki comparison
Hashimoto, S., et al. (2010) Solid State Ionics 181(37-38): 1713-1719

## Slide 17: Chemical capacitance calculation
Definition of capacitance
For charged species with charge , charge stored is
We then define chemical capacitance as the change in charge in response to a change in electrochemical potential
Where is the electrochemical potential and
At equilibrium and electroneutrality for electrons, oxygen vacancies, and neutral oxygen we have
So we can rewrite
which is larger when changes by a greater amount with changes in oxygen partial pressure
If follows a power law dependence with , we can integrate from a reference and to get
Notes: i.e. change in charge stored on e.g. a parallel plate capacitor with change in applied potential

## Slide 18: Calculation with Cchem data

## Slide 19: Maier comparison
Baumann, F. S., et al. (2006) Solid State Ionics 177(11-12): 1071-1081
Baumann, F. S., et al. (2007) Journal of the Electrochemical Society 154(9): B931-B941
LSC
LSF

## Slide 20: Film comparison
Our dots
  250nm thick, < 5nm rms roughness
  100-500µm diameter
Their dots
  100nm thick, look much rougher
  60-80µm diameter (3PB contribution?)
Baumann, F. S., et al. (2006) Solid State Ionics 177(11-12): 1071-1081
electrolyte (YSZ, BZY…)
porous, high-activity counterelectrode
Heated stage
Al2O3

## Slide 21: (100) YSZ resistance
Newman equation
For 125 µm diameter dot at 700°C
  Roffset ≈ 10kΩ implies
  Implies temperature closer to 675°C
  May over-weight lower (hotter) section of YSZ
Newman, J. (1966) Journal of the Electrochemical Society 113(5): 501-&.
700°C
1 atm O2

## Slide 22: Conclusion
Accurate temperature calculation is vital to complete understanding & comparison to existing results
  Pyrometer
  Surface thermocouple
  Temperature-indicating lacquers
  Buried/pressed thermocouple
  Next: use Pt paste and Pt-Pt/Rh wires to make a true “surface” thermocouple
Otherwise, data look fantastic!
Next steps:
  WDS characterization & composition confirmation
  New materials!

## Slide 23: Acknowledgements
Dr. Sihyuk Choi
Yangang Liang & Dr. Xiaohang Zhang (UMD)
Professor Ichiro Takeuchi (UMD)
Professor Sossina Haile